## Slide 1: FXCN - REWORK BGA FLOWCHART
Baking the board
Close return boards to product line
6.Place PCBA into machine
12. Close return board to
Product line
10. Measure, X-ray, ICT, FT
11. Send out weekly scrap report to customer
1. FXCN
suspect failure detect by BGA
FXCN suspect failure error code related BGA(SoC)
Place PCBA into machine and setup temperature parameters (RE)
Remove BGA, Clean BGA Pad (RE)
Place New BGA into PCBA and Solder by machine (RE)
Measure, X-ray, ICT, FCT
Summary Scrap weekly report to customer (RE)
Inspecting component after baking (RE)
9. Place new BGA into PCBA and
solder by machine
Visual Inspection BGA PAD under microscope(RE)
8. Visual Inspection BGA PAD under
microscope
Send list units fail to SPE approval(PE/PM)
Customer approved change BGA
2. Send list units fail to SPE
approval
3. Customer SPE approved
Fail
Pass
Check in
Check Out
Production line
IN RE room
IN RE room
Check in
Check Out
RE area
Production line area
Data Procedure
4. Baking the board
5.Inspecting component after baking
7. Remove BGA, Clean BGA PAD